IT4Innovations 8th Open Access Call
To be submitted before: 2016-07-27 23:59:59

Name of the project: Ab initio study of core electron binding energy shifts in amorphous Ti1–nSinO2
Number of core hours requested: 193600
Name and surname of primary investigator:Pavel Ondračka
Affiliation of primary investigator:Department of Physical Electronics, Faculty of Science, Masaryk University (PhD student, Advanced Materials and Nanosciences program)
Central European Institute of Technology, Masaryk University
e-mail: pavel.ondracka@gmail.com

Names and surnames of other investigators[1]: David Holec a, Lenka Zajíčková b,c
[1] Comma separated list
Affiliations of other investigator1:
a Department of Physical Metallurgy and Materials Testing, Montanuniversität Leoben
b Department of Physical Electronics, Faculty of Science, Masaryk University
c Central European Institute of Technology (CEITEC)
e-mail1: david.holec@unileoben.ac.at, lenkaz@physics.muni.cz

Research area: Materials Science, Physics

Popular abstract:
Mixed Ti1–nSinO2 materials offer interesting optical properties due to the high difference between refractive indices (TiO2: ~2.5, SiO2: ~1.5) and band gaps (TiO2: ~3.2 eV, SiO2: ~8.5 eV). Mixing of SiO2 and TiO2 is a perspective way how to alter the dielectric constant and refractive index, and simultaneously improve insulating properties. This opens new possibilities in designing optical devices such as multilayer antireflective coatings, interference filters, or waveguides.
Regardless of its exciting properties, the current material quality of Ti1–nSinO2 thin films still limits their performance. An important property of Ti1–nSinO2 is its structure, especially whether the distribution of Ti and Si atoms is homogeneous (i.e., they are perfectly mixed in a common network) or, on the contrary, there are zones enriched in silicon or titanium oxides. X-ray photoelectron spectroscopy (XPS) can be used to determine the TiO2/SiO2 mixing from the shifts of photoelectron energies. However, the data analysis is not straightforward and may be ambiguous without sufficient theoretical understanding.
Modern computational methods can guide experiments by providing materials trends and selection rules and thus reduce significantly the experimental efforts and costs. In particular, quantum-mechanical calculations based on the Density Functional Theory provide highly accurate and affordable predictions. Utilization of the computational power provided by the Salomon supercomputer will enable the calculation of XPS spectra of amorphous mixed Ti1–nSinO2 material in the whole compositional range from TiO2 to SiO2 The results will serve as a reference for the XPS data evaluation and subsequent experimental work focused on further application-oriented material development.
Scientific readiness:
Aims and objectives
The aim of this project is to calculate XPS spectra of Ti1–nSinO2 amorphous phase for different n values covering the whole compositional range from TiO2 to SiO2 as well as XPS spectra of selected TiO2 and SiO2 crystalline polymorphs. Core states of interest will be O 1s, Ti 2p and Si 2p, which are common choices in experimental studies. The main objective is to observe trends in the shifts of the XPS peaks, and use them for interpreting fitted experimental XPS spectra. X-ray photoelectron binding energies for individual atoms will be evaluated together with their chemical surrounding and this will help to better understand the nature of Ti1–nSinO2 core states energy shifts.
This project is a follow up of the project OPEN-6-17, which focused on the same topic. In the framework of OPEN-6-17 XPS spectra were calculated for 7 selected compositions and were found in good agreement with experimental data, hence validating the used methodology. However, due to the small number of the calculated structures, it is unclear if some observed minor trends in the calculated data have physical origin or are just artifacts due to the limited cell size and randomness of the simulated annealing procedure. Hopefully by doubling the number of calculated structures, those questions can be properly resolved.
Methods and state-of-the-art
Structural models of Ti1-nSinO2 amorphous materials will be generated using a supercell-based ab initio Molecular Dynamics technique called “simulated annealing” . The amorphous cell generation and subsequent structural optimization will be done using co-investigater’s computational resources. The cell sizes will be in a range of around 100 atoms as a compromise between having an infinitely large amorphous cell and making the study computationally feasible. The quantum mechanical calculations will be performed within the framework of Density Functional Theory (DFT) [2,3], which replaces a solution of the Schrödinger equation for many-body wave-function with a search for the corresponding charge density. An all-electron fully relativistic DFT package WIEN2k will be used in this project. It is based on the full-potential (linearized) augmented plane-waves + local orbitals method [4], one among the most accurate schemes for band structure calculations. Standard generalized gradient approximation for the exchange and correlation functional parametrized by Perdew, Burke and Ernzerhof (PBE) will be used [5].
Two methods for calculation of XPS binding energies of localized orbitals such as the core-level states will be evaluated and used:
ΔSCF method [6]: The binding energy Eb is defined by the energy difference between the state with N − 1 electrons and that with N electrons: Eb = E (N − 1) − E (N). In the N − 1 electron system, a hole occupies the core-level state and the emitted electron is located at infinity.
Slater transition state method [6]: where the binding energy Eb is calculated as the eigenvalue ε of state with one half electron removed. Eb = ε(N – ½).
Analysis of the atomic surroundings and bonds will be done using the Atoms in molecules (AIM) theory [7].
 Impact and outlooks
The most common way to prove presence and amount of Ti–O–Si bonds is the identification by the intensity of an infrared (IR) absorption band between 900 and 965 cm−1 in IR spectroscopy [8-10]. This approach however have some serious issues. It depends on the infrared absorption cross-sections that are different for Ti–O–Ti, Si–O–Si , and Si–O–Ti bonds. While the first two can be determined from pure TiO2 and SiO2 respectively, this is not possible for Si–O–Ti and hence needs to be fitted. Additionally, this method assumes constant absorption cross-sections for different compositions of Ti1–nSinO2, which is not the case when mixing materials with big refractive index differences.
On the contrary, XPS does not suffer from these issues, however accurate fitting of XPS spectra is difficult and peak positions must be often fixed by hand to obtain reasonable results. A thorough analysis of the calculated XPS spectra can help the experimental data fitting by providing estimates for the peak positions as predicted by the ab initio calculations. Since no ab initio study concerning XPS of Ti1–nSinO2 has been published up to date, the here proposed work is a novel approach to this issue.
Computational readiness:
Computational approach, parallelization and scalability:
WIEN2k software used for this project is written in FORTRAN90 and requires a UNIX system (programs are linked together via C-shell scripts). The applicant owns a valid academic license. WIEN2k does not require any special libraries, but it uses optimized BLAS and LAPACK libraries if present. It is mostly tested and optimized for the Intel proprietary compiler, but can be built with GNU compiler collection as well.
WIEN2k has a built-in parallelization scheme (so-called k-point parallelization), where subsets of the k-point mesh (sampling the Brillouin zone) are distributed to different processors, and subsequently combined. There are some parts of the main self-consistent file (SCF) cycle which are not parallelized, however their computational costs are negligible compared with the rest of the cycle.
Additionally, MPI fine-grained parallelization can be used when necessary, e.g., for memory limited problems or where there are fewer k-points than available processors.
One typical SCF cycle on a test 96-atom amorphous unit cell takes approximately 10 CPU-hours, out of which only few seconds are pure serial code, and the rest makes use of the built-in k-point parallelization scheme.
Computational resources:
Requested resources were estimated from older computation of amorphous unit cell with 96 atoms cell size and 3x3x3 k-points grid done on Salomon cluster as a part of project OPEN-4-7.
Planned amount of calculated structures: 6
Calculations per structure: 128 (64 x O 1s + 32 * (Ti/Si 2p1/2 and 2p3/2)
Usual number of SCF cycles needed to converge a calculation : 15-20
Core hours needed for one typical cycle with 96 atoms cell size: 10
Additional core hours needed for larger test cases (to test cell-size effects), convergence tests, safety margin, and for post-processing analysis (such as AIM calculations): 40000
Total CPU hours needed: 6 * 20 * 10 * 128 + 20000 = 193600
Economic readiness:
Socioeconomic impact:
Improvements in XPS characterization enabled by this work will lead to higher quality and improved performance of Ti1–nSinO2 films.
In a long run, this research could lead to a development of novel components such as multilayer antireflecive coatings, interference filters, or waveguides with greatly improved optical performance.
Outside of optical application, another widespread use for TiO2 and Ti1-nSinO2 oxides is in photocatalysis, with applications including self-cleaning surfaces, air and water purification systems, sterilization, hydrogen evolution, and photoelectrochemical conversion.
Operational costs:
This work will be done in parallel to experimental studies performed within the frameworks of funded projects of the CEITEC Plasma Technologies group (group leader Prof. Lenka Zajíčková). The calculations will be done within the PhD project of Pavel Ondračka (principal investigator of this proposal), whose scholarship is paid from the Masaryk University and CEITEC resources. There are no other financial resources available for the PI to cover the operational costs related to the use of the supercomputer.
Amortization and renewal:
As described above, there are unfortunately no free financial resources available towards amortization and renewal of the cluster hardware.
References:
[1] A. Zunger, S.-H.Wei, L.G. Ferreira, and J. E. Bernard, Phys. Rev. Lett. 65,(1990)
[2] W. Kohn and L. J. Sham, Physical Review 140, A1133–A1138 (1965).
[3] P. Hohenberg and W. Kohn, Physical Review 136, B864–B871 (1964).
[4] G. K. H. Madsen, P. Blaha, K. Schwarz, E. Sjöstedt, and L. Nordström, Phys. Rev. B 64, 195134 (2001).
[5]J. P. Perdew, K. Burke, and M. Ernzerhof, Phys. Rev. Lett., 77:3865–3868 (1996).
[6] R. M. Martin: Electronic Structure, Cambridge University Press (2004).
[7] R. Bader, Chemical Reviews 91: 893¨C928. (1991).
[8] M. Landmann, T. Köhler, E. Raus, T. Frauenheim and G. W. Schmidt, J. Phys.: Condens. Matter 26, 253201 (2014).
[9] F. Gracia, F. Yubero, J. Holgado, J. Espinos, A. Gonzalez-Elipe, and T. Girardeau, Thin Solid Films 500, 19 (2006).
[10] S. Larouche, H. Szymanowski, J.E. Klemberg-Sapieha, L. Martinu, and S. C. Gujrathi, Journal of Vacuum Science & Technology A: Vacuum, Surfaces, and Films 22, 1200 (2004).